|  | Product Data Sheet |  |
| --- | --- | --- |
| FOAMED POLYSTYRENE BOARD – PAPER COATED Page 1 of 1 This is a UK manufactured expanded Polystyrene foam cored board laminated on both sided with white coated paper treated with an anti UV coating. It is fairly strong but is better used inside and not in wet or windy conditions. It is CFC Free so is more environmentally friendly than Foamed PVC which when burned evolves dioxins which are highly toxic. This can be safely disposed of with standard waste. CHARACTERISTICS Thickness: 3mm 5mm 10mm Density: 0.53 g/m² 0.56 g/m² 0.76 g/m² Width & Length Tolerances: +or – 2mm Square Fault: Max: 4mm per 1000mm Foam and Paper Colour: White Ageing: Treated with anti-Ultra Violet for protection against sunlight. Paper pH: 7.5 – 9.5 PROPERTIES Cutting: Cut with a simple cutter or an industrial die cutter. Printing: Can be screen printed or used directly on digital printers, compatible with all current inks. Lamination: Manual or industrial lamination – dry or humid (without solvent glue) Cold or warm (max temp. for all warm uses: 500C). Any questions please just ask. APPLICATIONS: Internal Applications: Due to paper coating best used indoors. Media & Communications: Advertising and photo mounting Models construction: Architects, designers and artists Framing: Poster Manufacturing: General uses in industry, schools and leisure clubs. Decoration & Advertising: Shop – window dressing and making advertising displays. STORAGE: Flat. Not behind windows (magnifying glass) in a 300C maxi warehouse. eSheet Limited. 49 Oakhurst Close, Belper. Derbys DE56 2TR Tel: 01773 823556 Fax: 01332 440200 Email sales@esheet.co.uk Web: http//:www.esheet.co.uk This data is derived from typical sample test pieces from various sources and should not be relied on for any commercial purpose. If exact information is required then please contact us. 06/11/10 |